Table 1. Characteristics & Chemical Analysis of Samples, Reconnaissance Visit to

ITOK GmbH Gold Resources in Dinguiray, Guinea, 27-31 May 2009

| ITEM | Sample No. | Zone No. | Location | Coordination |  | Sample Description | Au | Ag | Cu | Mo | Pb | Sn | Zn | B |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Latitude | Longitude |  | PPM | PPM | PPM | PPM | PPM | PPM | PPM | PPM |
| 1 | DS1 | Zone 2 | 1 Km North-East of Kourufing Village | N11 38 43.4 | W10 33 49.4 | Taken from weathered soil, semi-washed | 9.500 | 0.29 | 61 | 1.4 | 39.0 | 1.3 | 168 | 7.5 |
| 2 | DS2 | Zone 2 | 1 Km North-East of Kourufing Village | N 11 38 46.8 | W10 33 47.1 | Taken from raw weathered soil | 0.320 | 0.13 | 52 | 0.7 | 9.3 | 2.4 | 76 | 153 |
| 3 | DS3 | Zone 2 | 1 Km North-East of Kourufing Village | N11 38 29.3 | W10 33 43.4 | Taken from raw weathered soil | 33.100 | 0.74 | 48 | 2.9 | 765 | 1.9 | >1000 | 168 |
| 4 | DS4 | Zone 1 | 3 Km South of Rogaya Village | N11 43 00.7 | W10 29 40.5 | Taken from raw weathered soil | 1.380 | 0.44 | 60 | 1.8 | 41.0 | 3.6 | 213 | 19 |
| 5 | DS5 | Zone 1 | 3 Km South of Rogaya Village | N11 43 00.7 | W10 29 40.5 | Taken from concentrate, traditional washed | >100 | 6.70 | 43 | 13.0 | 760 | 100 | 440 | 7.1 |
| 6 | DS6 | Zone 1 | 3 Km South of Rogaya Village | N11 42 50.9 | W10 29 41.2 | Taken from dig | 0.034 | 0.39 | 320 | 2.1 | 7.0 | 1.5 | 20 | 12 |
| 7 | DS7 | Zone 1 | 3 Km South of Rogaya Village | N11 42 50.9 | W10 29 41.2 | Taken from dig | 0.058 | 0.22 | 77 | 2.1 | 12.0 | 3.7 | 66 | 13 |